TAP 228- 3: Materials database

Here are data for about a dozen properties of some 50 materials in Excel spreadsheet format.  You can create lists ordered by property, search for materials with properties in certain ranges, etc. To compare pairs of properties, it is best to use the selection charts.

If you double click on the chart below it will open as an Excel spreadsheet that can be copied and used.

Possible uses of the spreadsheet:

1.	Simple reference source for materials data – e.g. to solve quantitative problems involving materials selection, e.g. perhaps calculate the necessary thickness for required thickness or strength of a cantilever.

2.	Sort by property, e.g. which are the ten toughest materials in the database?

3.	Search with logical operators, e.g. find all materials in the database stiffer than X, stronger than Y, less dense than Z.  Try doing this by reading the information from a couple of charts.

4.	Explore combinations of material properties not provided as selection charts – e.g. plot modulus against strength.  Note that single 'typical' values are provided in the database rather than the full range, so this does give a true selection chart, but can identify interesting trends.

5.	Design problems often lead to combinations of properties for which high or low values are required.  A common example is 'specific stiffness' (the Young modulus divided by density), which gives an indication of materials which are light and stiff.  Specific stiffness and strength are shown in one of the selection charts.  Other compound properties for particular design problems could be calculated and plotted using the spreadsheet.

Also provided, below is a data that provides definitions of the materials in the database, and summarises their strengths and weaknesses in engineering design, typical applications and environmental notes. This is a useful reference source for materials.  Not all will be needed.

Materials information

Double click on the icon below to access a materials database.  This is an html document and will activate internet explorer.  It has been virus checked.

Practical advice

This database has many potential uses e.g. comparison of experimental values.

Alternative approaches

Data books may be used to augment the information provided here. It has been deliberately provided in an open format.

Social and human context

The ability to search, sort and calculate adds value to raw data.

External References

This activity is taken from Advancing Physics Chapter 4, file 10D